## Slide 1: Highly Recycled Asphalt Pavement
Martins Zaumanis
31.12.2023

## Slide 2
Annually 750,000 t of Reclaimed Asphalt Pavement (RAP) are not re-used in Switzerland

## Slide 3: Objective
Develop recommendations that would allow increasing the average reclaimed asphalt content in asphalt production without compromising the pavement performance.

## Slide 4: HighRAP project overview
Participants
Sponsors
Bundesamt für Strassen Bundesamt für Umwelt AWEL Kanton Zürich ANU Kanton Graubünden
Duration: 06.2019-12.2022

## Slide 5
Project participants
Principal investigator
Martins Zaumanis, Empa, Concrete and Asphalt Laboratory
Participants
Lily Poulikakos, Empa, Concrete and Asphalt Laboratory
Lukas Boesiger, Ammann Schweiz AG
Bernhard Kunz, BHZ AG
Henry Mazzoni, Catram AG
Peter Bruhin, Catram AG
Dominique Lötscher, Reproad AG
Urs Schellenberg, Kanton Zürich
Voluntary Contribution
Gion Dosch, Tiefbauamt Graubünden
Gabriel-Martin Elekes, TBA Graubünden
Viele andere
Monitoring committee
President
Fabian Traber, Bundesamt für Strassen (ASTRA)
Participants
David Hiltbrunner, Bundesamt Für Umwelt (BAFU)
Remo Fehr, Amt für Natur und Umwelt - Kanton Graubünden
Dominik Oetiker, Amt für Abfall, Wasser, Energie und Luft – Kanton Zürich
Christoph Gassmann, Baudirektion Kanton ZH Tiefbauamt
Nicolas Bueche, Bern University of Applied Sciences (BFH)

## Slide 6
RAP Material: RAP Processing

## Slide 7: Four different crushers were used for the experiment

## Slide 8
Chunk Index demonstrates the size of RAP agglomerations.
Breakdown Index demonstrates the reduction of RAP aggregate particle size during processing.
Filler Increase Index reflects the amount of generated filler content during RAP processing.
Three indexes that allow evaluating crushing and screening of RAP were developed:

## Slide 9: The indexes can be determined using gradation analysis of RAP before and after binder extraction.

## Slide 10: A radar chart allows comparing different RAP crushing methods and optimize the crusher parameters
Smaller area = better RAP processing

## Slide 11: Calculator is available for download: https://doi.org/10.5281/zenodo.5500154

## Slide 12
RAP Material: RAP milling

## Slide 13: Why do we need to research milling?
Milling is most often viewed from the process perspective, for example by optimizing pavement removal speed, milling depth, machine wear, energy use, and other parameters.
There is almost no research on how milling affects the RAP properties.
RAP is an important material for asphalt production.

## Slide 14
The idea: Milling parameters impact the RAP properties. But which parameters and how?

## Slide 15: Result: milling does not age binder
(illustration courtesy of Wirtgen)

## Slide 16: Result: The aggregate angularigy is not impacted by milling

## Slide 17: Result: The size of RAP agglomerations increase with higher milling speed
9-F-20 (Chunk Index = 23.5%)
4-M-26 (Chunk Index = 14.3%)
7-S-20 (Chunk Index = 20.5%)
12-M-19 (Chunk Index = 28.9%)

## Slide 18: Result: less filler is generated at lower milling speed

## Slide 19
RAP Material: RAP Characterization

## Slide 20: Fragmentation test
Recommended by RILEM
Tested at 20 °C
150 mm molds
56 Blows (5 layers)
3 kg of material
Result = Passing through control sive (PCS), %

## Slide 21: Cohesion test
Recommended by RILEM
RAP compacted at 140 °C using gyratory compactor (150 mm mold)
Indirekt Tensile Test at 25 °C
Result = Indirect tensile strength
Result = NflexFactor

## Slide 22: Result Summary
None of the tests is ready for implementation
Further research is necessary
Fragmentation test
High Repeatability
Sensitive to RAP processing method
Effect of RAP agglomerations and aggregate toughness could not be established
Cohesion test
Sesntive toward bitumen softening point
Sensitive toward bitumen aging
Not sensitive toward bitumen content

## Slide 23
RAP-Variability
Tasks | Activities during HighRAP project
Determine the impact of RAP homogeneity | A theoretical calculation to determine the impact of RAP homogeneity based on the RAP content in mixture

## Slide 24: Assumed RAP variability (but representative of praxis)
Calculation of bitumen penetration
Calculation of rejuvenator effect

## Slide 25: Variability of RAP binder penetration depending on the RAP content

## Slide 26: RAP variability calculator available: https://doi.org/10.5281/zenodo.7441805

## Slide 27
Mix design: Rejuvenators

## Slide 28: Rejuvenator dosage to reach the penetration of target grade
Step 1:

## Slide 29: Determine aging resistance
Step 2:
1) Mass change after RTFO aging
2) Penetration after RTFO + 2PAV

## Slide 30: Calculator for determining dosage: https://doi.org/10.5281/zenodo.7441805

## Slide 31
Mix design: Performance-based design

## Slide 32
Drawing Author: Martins Zaumans
Rutting resistance:
Semi-Circular Bending test
Plastic deformations:
Cyclic compression test
Pass-fail criteria developed

## Slide 33: Example optimization of bitumen content

## Slide 34: Performance-based mix design
Optimize the rejuvenator content for the mixtures based on target penetration results.
Use a cracking test and a plastic deformation test to balance the design binder content and other design parameters.
As needed, perform additional binder and mixture tests before approving the final designs.

## Slide 35
Test section: Uster

## Slide 36: Location

## Slide 37: Mix types
Reference
HighRAP

## Slide 38: RAP was heated to production temperature in Ammann asphalt plant
Rejuvenator added in the mixer
Production: BHZ AG Asphalt plant in Volketswil

## Slide 39
Video from construction
(https://youtu.be/MvyCwyrMNOs)

## Slide 40
The produced mixtures were thoroughly characterized using mixture and binder tests

## Slide 41: Summary

## Slide 42
· 30 % RAP used in wearing course with good performance in PmB 45/80-80 grade; with 60% RAP not possible to reach this grade
· 40-50 % RAP likely allows to reach PmB 45/80-65 grade
· 65% RAP used in unmodified binder course—with good performance
Summary

## Slide 43
Test section: Lukmanierpass

## Slide 44: Location

## Slide 45: Mix types

## Slide 46: RAP heated to production temperature using Contimix RAH 100% and Ammann Universal 300
Rejuvenator added on cold RAP
Production: Catram AG asphalt plant in Untervaz

## Slide 47
ACF22 85 HighRAP
AC T 16 85 Ref
ACF22 125 (1) HighRAP
Sample collection

## Slide 48: 1 year after construction: no problems

## Slide 49
The produced mixtures were thoroughly characterized using mixture and binder tests

## Slide 50: Summary

## Slide 51
· 85 % RAP was used in foundation course mixtures with good performance
· 60-70 % RAP was used in base course with good performance
· Good thermal cracking resistance for all mixtures
Summary

## Slide 52
Recommendations

## Slide 53: Recommendations
· Use RAP ≤30 % in PmB wearing course (PmB 45/80-80) and ≤50 % in PmB base/binder course (PmB 45/80-65)
· Use RAP in high altitude ≤ 70 % in base/binder course and ≤85 % in foundation course
· (Higher RAP contents can be considered with proof of performance)
· Permit high RAP use only if high RAP homogeneity of RAP is ensured (especially binder content & properties)
· Use performance-based mix design for type testing (testing of cracking resistance is especially important)

## Slide 54: Recommendations
· Select rejuvenator dosage based on target penetration
· Approve rejuvenator/soft binder by testing aging resistance (RTFO+2xPAV): test mass loss & penetration
· Ensure correspondence to conventional extracted binder & mixture test requirements
· Consider MSCR binder test for RAP use in PmB mixtures
· Use CBF indexes to optimize RAP crushing and screening
· Implement these recommendations after local validation

## Slide 55
All results

## Slide 56
https://www.empa.ch/web/s308/highrap
This Presentation
Report &
summary in DE, FR, EN
One-pager
Download
Excel-spreadsheets
Results of the HighRAP-Project
Contact: martins.zaumanis@empa.ch